## Slide 1: Actinic inspection of logic patterns using coherent diffraction imaging at high NA
Iacopo Mochi, Patrick Helfenstein, Rajendran Rajeev, Sara Fernandez, Dimitrios Kazazis and Yasin Ekinci

## Slide 2: Outline
RESCAN – A platform for actinic pattern inspection
Description.
Working principle.
Latest performance highlights
Programmed defect detection on logic patterns.
Through-pellicle inspection.
Virtual through-focus mask inspection.
Resolution and throughput
Performance test of the EUV-optimized JUNGFRAU detector
Outlook and future plans

## Slide 3: RESCAN
60 cm
EUV reticle
Coherent EUV
illumination
Detector
Actinic pattern inspection platform based on CDI
Synchrotron-based
Tunable wavelength
  EUV optimized
λ/∆ λ ≈ 1500
Max sample size: 2×2 cm2
Inspection area: 200x200 μm2
NAmax: 0.24
Resolution limit: 34 nm
Compact vacuum chamber
XIL-II beamline SLS

## Slide 4: Programmed defect in a random pattern
Variable size extrusion defects
Pattern CD: 200 nm (on mask)

## Slide 5: Pattern comparison for accurate defect localization
μm
Reference
μm
200-nm extrusion
Defect map
Reconstructed area: 20×20 μm2.
Average iteration time: 80 ms.
Defect SNR: 15
Die to die defect inspection:
comparing a defect free area of the sample to a defective one.

## Slide 6: A practical approach: die to database inspection
Comparison between reconstructed image and mask design.
200×200 nm2 extrusion defect.
μm
μm
Apply spatial frequency filter to reticle design.
Calculate the best fitting affine transformation matrix.
Align and compare the images
Mask layout
Ideal mask image
Reconstructed amplitude image
Defect map

## Slide 7: Close to the resolution limit
200×200 nm–SNR 7.3
150×200 nm–SNR 6.2
100×200 nm–SNR 5.2
50×200 nm–SNR 6.5
μm
μm
μm
μm
Defects down to 50×200 nm (on mask) are detected with a significant SNR.
The current resolution limit of RESCAN is 34 nm.
Notes: To help the defect visualization we can threshold and binarize the images.

## Slide 8: Closer to the resolution limit
Die to die inspection of an industry-standard 70-nm TaBN absorber mask.
CD: 115 nm. Defect size: 141×35 nm
SNR: 8.1

## Slide 9: Exploring the through-focus behavior of the sample
Post-processing reconstruction of a tilted sample
Through-focus pattern inspection
Phase structures contrast enhancement
1.5 μm
1.5 μm

## Slide 10: Through pellicle EUV lensless imaging
No pellicle
Si3N4 membrane(100 nm)
SW-CNT pellicle
Pellicles mounted statically: the illumination beam goes through the same spot on the pellicle and the sample moves underneath at a distance of 4 mm.
Pellicle
Reticle
The CNT pellicles withstood 6.8h of EUV illumination inside the RESCAN chamber without visible damage and without degradation in the imaging performance.
MW-CNT pellicle
Pressure: 2⋅10-8 – 2⋅10-7 mbar.
Power densitymax: ~3 W/cm2.
λ\dλ : 1500.
No pellicle
Si3N4 membrane
(100 nm)
SW-CNT pellicle
MW-CNT pellicle
1.5 μm

## Slide 11: Planned upgrades and roadmap
From EUV CCD to two-modules EUV-optimized JUNGFRAU detector.
Large dynamic range
Single acquisition and short exposure time (<0.01 s).
High NA
Resolution limit down to 20 nm.
EUV CCD
Pixel size: 13.5 μm.
Acquisition frame rate: 1 Hz.
Dynamic range: 16 bit
NA: 0.24
Pixel number: 2048×2048
JUNGFRAU
Pixel number: 1024×512 (1 module)
Pixel size: 70 μm.
Acquisition frame rate: 2000 Hz.
Dynamic range: 20 bit.
NA: 0.4

## Slide 12: Data acquisition with the JUNGFRAU detector
EUV image profile of the diffraction pattern generated by a grating.

## Slide 13: Summary
RESCAN can effectively map programmed defects on periodic and non periodic patterns.
Die-to-die and die-to-database inspection modes are available.
We are upgrading RESCAN with a high NA detector that will enable defect inspection down to 20 nm.
We demonstrated defect inspection down to 35 nm (on mask) with a high SNR.
RESCAN latest results.
We started testing RESCAN with EUV pellicles.
Planned upgrades.
Analysis of programmed phase defects on logic patterns.
Further investigation of the impact of pellicles on defect inspection.

## Slide 14: Wir schaffen Wissen – heute für morgen
Acknowledgements
PSI
Michaela Vockenhuber
Marcus Kropf
Aldo Mozzanica
Sophie Redford
Zuhal Tasdemir
Pellicles and membranes
Emily Gallagher (IMEC)
Marina Timmermans (IMEC)
Lintec, NSTC
Canatu Oy
TaBN samples
Shusuke Yoshitake (NFT)
Shingo Yoshikawa, (Dai Nippon Printing Co., Ltd.)